聚乙烯（HDPE）给水管

HDPE pipe for water supply

产品介绍

聚乙烯给水管是以高密度聚乙烯（HDPE）树脂为原料，采用复合挤出成型工艺加工而成的一种新型管道产品，是传统的钢铁管材、聚氯乙烯饮用水管的换代产品。具有质轻、柔韧性好、耐腐蚀、抗冲击性能优良等优点。广泛应用于市政给水、消防、工业、农业、矿山、油田等各类输水工程，以及泥浆、砂浆输送，电力电信线缆保护套管等用途。

管材规格范围dn20-dn1600mm,压力范围0.4MPa-2.0MPa。

产品特点

1、耐老化，正常条件下使用寿命达50年以上。

2、卫生性好，无毒、不含重金属,无结垢层，不滋生细菌。

3、耐腐蚀，可耐多种化学介质的腐蚀：无电化学腐蚀。

4、内壁光滑阻力小，摩擦系数低，介质通过能力强。

5、柔韧性好，抗冲击强度高，耐强震、扭曲。

6、耐磨性好，抗磨损，更长的使用寿命。

7、重量轻，运输、安装便捷，施工方便，工程综合造价低。

product description

Polyethylene pipe water supply is a new type of pipe product made of high-density polyethylene (HDPE) resin and processed by composite extrusion molding technology. It is a replacement product for traditional steel pipes and PVC drinking water pipes. It has the advantages of light weight, good flexibility, corrosion resistance and impact resistance. Widely used in municipal water supply, fire protection, industry, agriculture, mines, oil fields and other water delivery projects, as well as mud and mortar transportation, dredging, power and telecommunication cable protection casings, etc.

Pipe specification dn20-dn1600mm, pressure 0.4MPa-2.0MPa.

Features

1. Aging-Resistance, with a service life of more than 50 years under normal conditions.

2. Good sanitation, non-toxic, no heavy metals, no scaling layer, no bacteria breeding.

3. Corrosion resistance to various chemical media, no electrochemical corrosion

4. Low friction coefficient, and strong medium passing capacity.

5. Good Flexibility, high impact strength, strong shock and twist resistance.

6. Wear resistance and longer service life.

7. Light weight, convenient transportation and installation, low construction cost.

HDPE钢丝网骨架复合管

Steel Wire Reinforced HDPE Composite Pipe

产品介绍

HDPE钢丝网骨架复合管(简称SRTP），是以包覆处理后的高强度钢丝连续缠绕网成型的芯层为增强骨架，采用专用热熔胶粘接树脂、聚乙烯通过连续挤出成型方法复合成一体的新型环保管材。它既保留了钢管优良的承压性能，又保留了塑料管良好的卫生性能以及易于敷设、技术可靠、使用寿命长等特点。广泛适用于市政和建筑的给水、消防管网和气体输送，亦可运用于化工、石油、医药等工业介质的输送。

管材规格范围dn50-dn800mm,压力范围0.8MPa-3.5MPa。

产品特点

1.具有更高的承压强度和抗蠕变性能。

2.具有超过普通纯塑料管的刚性、抗冲击性，类似钢管的低线膨胀系数。

3. 内壁光滑，不结垢，水流摩擦阻力小，输水能力大。

4. 耐腐蚀性好，管材内外层为塑料层，具有与塑料管相同的优良防腐性能。

5. 重量轻，装卸运输方便。

6. 采用电熔连接，施工快捷方便，接头不渗漏。

7. 抗磨损性能良好，在正常使用情况下，使用寿命50年。

product description

HDPE Steel Wire Mesh Composite Pipe (SRTP for short) is based on the core layer formed by the continuous winding of high-strength steel wire after coating treatment as the reinforced skeleton, and is compounded with special hot-melt adhesive resin and polyethylene through continuous extrusion molding Integrate new environmental friendly pipes. It not only retains the excellent pressure-bearing performance of steel pipes, but also retains the good hygienic performance of plastic pipes, easy laying, reliable technology, and long service life. It is widely used in municipal and building water supply, fire pipe network and gas transportation, and can also be used in the transportation of chemical, petroleum, pharmaceutical and other industrial media.

Pipe specification dn50-dn800mm, pressure 0.8MPa-3.5MPa.

Features

1. Higher compressive strength and creep resistance.

2. Rigidity and impact resistance higher than ordinary plastic pipes, low linear expansion coefficient similar to steel pipes.

3. The inner wall is smooth, no scaling, small frictional resistance of water flow, large water delivery capacity.

4. Good corrosion resistance, the inner and outer layers of the pipe are plastic layers, which have the same excellent anti-corrosion performance as plastic pipes.

5. Light weight, easy to load, unload and transport.

6. The electric fusion connection is adopted, the construction is quick and convenient.

7. Good anti-wear performance, service life is 50 years under normal using conditions.

UPVC给水管

UPVC Pipe for Water Supply

产品介绍

硬聚氯乙烯（UPVC）给水管道作为一种发展成熟的供水管材，以卫生级聚氯乙烯树脂为主要原料，添加定量的添加剂，经塑料挤出机挤出成型而生产出的一种给水用管材。具有耐腐蚀性强，耐压性能好，流体阻力小，符合卫生要求，施工方便等优越性能。广泛应用于城乡供水排水管网，工业，农业灌溉、凿井等工程及其他工业用管。

管材规格范围dn20-dn1200mm,压力范围0.5MPa-2.5MPa。

产品特点

1、质轻，搬运装卸、施工方便。

2、具有优异的耐酸、耐碱、耐腐蚀性。

3、内壁光滑，流体阻力小。

4、具有良好的耐压性能、抗冲击性能和抗拉伸强度性能。

5、连接施工迅速容易，施工工程费低廉。

product description

Rigid polyvinyl chloride (UPVC)pipe, as a well-developed water supply pipe, is produced by extruding plastic extruder with sanitary grade polyvinyl chloride resin as the main raw material and adding quantitative additives. It has strong corrosion resistance, good pressure resistance, small fluid resistance, conforms to hygienic requirements, and is convenient for construction. Widely used in urban and rural water supply and drainage pipe networks, industrial, agricultural irrigation, sinking and other industrial using purpose.

Pipe specification dn20-dn1200mm, pressure 0.5MPa-2.5MPa.

Features

1. Light weight, convenient for handling, easy for construction.

2. Excellent acid and alkali resistance and corrosion resistance.

3. The inner wall is smooth and the fluid resistance is small.

4. Good pressure resistance, impact resistance and tensile strength.

5. The connection construction is quick and easy, and the construction cost is low.

# HDPE双壁波纹管

# HDPE Double Wall Corrugated Pipe

产品简介

HDPE双壁波纹管是以高密度聚乙烯为原料的一种具有闭环结构外壁和平滑内壁的新型轻质管材，具有重量轻、耐高压、耐老化、耐环境应力开裂、韧性好、具有优异的化学性能、施工快、寿命长等优点。在国内外都得到了广泛的应用，大量替代了混凝土管和铸铁管。广泛应用于市政排水排污，农业灌溉，通风、渗透、工业化工、通讯套管等领域。

管材规格范围dn110-dn1000mm,环钢度范围SN4-SN8。

产品特点

1、强度高、抗压、耐冲击性好。

2、产品具有良好的挠曲性能，可适应土壤的不均匀沉降;。

3、使用寿命长，地埋使用可达50年以上;

4、内壁平滑，摩阻小，通水能力强。

5、绿色环保，耐腐蚀、无污染。

6、质轻，便于搬运，施工方便，工程综合造价低。

product introduction

HDPE double-wall corrugated pipe is a new type of lightweight pipe with a closed ring-shaped outer wall and a smooth inner wall made of high-density polyethylene. It has light weight, high pressure resistance, aging resistance, environmental stress cracking resistance, and good toughness. Excellent chemical properties, fast construction, long life and other advantages. It has been widely used at home and abroad, replacing concrete pipes and cast iron pipes in large quantities. Widely used in municipal drainage and sewage, agricultural irrigation, ventilation, infiltration, industrial chemicals, communication casing and other fields.

The pipe specification dn110-dn1000mm, ring stiffness SN4-SN8.

Features

1. High strength, good compression resistance and impact resistance.

2. The product has good flexural properties and can adapt to the uneven settlement of the soil;

3. The service life is long, and the buried use can reach more than 50 years;

4. The inner wall is smooth, the frictional resistance is small, and the water passing ability is strong.

5. Environmental protection, corrosion resistance and no pollution.

6. Light weight, easy to carry, easy to construct, and low overall project cost.

钢带增强聚乙烯(PE)螺旋波纹管

Metal Reinforced Polyethylene(PE)Spiral Corrugated Pipe

产品简介

钢带增强聚乙烯（PE)螺旋波纹管（简称MRP）是以聚乙烯树脂为基体，用表面涂敷粘接树脂的钢带成型为波形作为主要支撑结构，并与内外层聚乙烯复合成整体，在生产线上通过缠绕、挤出复合成型的螺旋波纹管材。其内壁平直、外壁呈螺旋波纹状，它不仅具有一般波纹管的优点，而且具有金属管的高强度，弥补了过去较大直径塑料埋地排水管一般环刚度只能达到SN8的限制。广泛应用于市政地下排水、排污、雨水收集、输水、渗水、通风、线缆护套管等工程项目。

管材规格范围dn300-dn2400mm,环钢度范围SN8-SN16。

产品特点

- 耐酸碱性能优良，使用寿命长。

- 钢带采取"U"形结构，耐压，抗冲击性能优越。

- 管材在-60℃环境中不会被冻裂及膨胀漏水。

- 重量轻，连接方便，便于运输，施工方便。

- 内外壁光滑，摩擦系数小，排水速度快。

Metal reinforced polyethylene (PE) spiral corrugated pipe (MRP) is based on polyethylene resin, and the steel strip coated with adhesive resin on the surface is formed into a corrugated form as the main support structure, and is composited with inner and outer polyethylene. , a spiral corrugated pipe formed by winding and extruding on the production line. Its inner wall is smooth and its outer wall is spirally corrugated. It not only has the advantages of plastic corrugated pipes, but also has the high strength of metal pipes, which makes up for the limitation that the ring stiffness of large-diameter plastic drainage pipes can only reach SN8 in the past. Widely used in municipal underground drainage, sewage, rainwater collection, water delivery, water seepage, ventilation, cable sheathing and other engineering projects.

The pipe specification dn300-dn2400mm, ring stiffness SN8-SN16.

Features

1. Excellent acid and alkali resistance and long service life.

2. The steel belt adopts "U" shape structure, which has excellent pressure resistance and impact resistance.

3. The pipe will not be cracked by freezing and expand and leak in the environment of -60°C.

4. Light in weight, easy to connect, transport and save construct cost.

5. The friction coefficient is small, and the drainage speed is fast.

克拉管-聚乙烯缠绕结构壁

Polyethylene spirally enwound structure-wall pipe

产品简介

克拉管即热态缠绕成型高密度聚乙烯(HDPE)缠绕结构壁管。该管壁是以高密度聚乙烯树脂为主要原材料，采用热态缠绕型工艺，以聚丙烯(PP)单壁波纹管为支撑结构制成具有较高抗外压能力的特殊结构壁管材。具有重量轻、耐高压、耐老化、耐环境应力开裂、韧性好、具有优异的化学性能、施工快、寿命长等优点。广泛应用于埋地排水、排污工程。

管材规格范围dn200-dn2000mm,环钢度范围SN4-SN16。

特点：

1、强度高、抗压、耐冲击性好。

2、重量轻，便于运输，施工方便快捷，可降低施工费用

3、具有很好的柔韧性,又有很强的刚性和整体抗外压能力。

4、抗腐蚀、耐老化,使用寿命长。

5、内壁光滑，阻力小，输水量大。

product introduction

Polyethylene spirally enwound structure-wall pipe-B Type, is a hot winding high density polyethylene (HDPE) winding structure wall tube. The pipe wall is made of high-density polyethylene resin as the main raw material, adopts hot winding technology, and uses polypropylene (PP) single-wall corrugated pipe as the supporting structure to make a special structural wall pipe with high resistance to external pressure. It has the advantages of light weight, high pressure resistance, aging resistance, environmental stress cracking resistance, good toughness, excellent chemical properties, fast construction and long service life. Widely used in buried drainage and sewage projects.

The pipe specification dn200-dn2000mm, ring stiffness SN4-SN16.

Features:

1. High strength, good compression resistance and impact resistance.

2. Light weight, easy to transport, convenient and fast construction, which can reduce construction costs

3. It has good flexibility, strong rigidity and overall external pressure resistance.

4. Anti-corrosion, anti-aging, long service life.

5. The inner wall is smooth, the resistance is small, and the water delivery capacity is large.

UPVC排水管材

UPCV Drainage Pipe

产品简介

UPVC排水管是技术成熟的排水管系列产品，以聚氯乙烯树脂为主要原料，加入适量的稳定剂、润滑剂、填充剂、增色剂经挤出成型的塑料管材。产品有铸铁管无以比拟的长久寿命，耐腐蚀等优点；在施工上更有重量轻便于搬运安装以及连接简易等特点、广泛应用于民用建筑排水排污，化工排水排污，排雨水等领域。

管材规格范围dn50-dn630mm。

产品特点

1. 管材表面硬度和抗拉强度优，管道安全系数高。

2. 抗老化性好，正常使用寿命可达50年以上。

3. 耐腐蚀性能优良，适用于工业污水排放及输送。

4. 摩阻系数小，水流顺畅，不易堵塞，养护工作量少。

5. 施工方法简单，操作方便，安装效率高。

product introduction

UPVC drainage pipe is a mature technology pipe, extruded with polyvinyl chloride resin as the main raw material and added with an appropriate amount of stabilizer, lubricant, filler, and color enhancer. It has the advantages of long service life and corrosion resistance than cast iron pipes ; It is light in weight, easy to transport and connect in construction,widely used in civil building drainage and sewage, chemical drainage and sewage, rainwater and other fields.

The pipe specification dn50-dn630mm.

Features

- The surface hardness and tensile strength of the pipe are excellent, more safety.

- Good aging resistance, the normal service life can reach more than 50 years.

3. Excellent corrosion resistance, suitable for industrial sewage discharge and transportation.

4. The friction coefficient is small, smooth water flow and the maintenance easy.

5. The connection is convenient, and the installation efficiency is high.

HDPE 地源热泵管

HDPE Pipe for Geothermal Heat Pump System

产品简介

HDPE地源热泵专用管材是以优质聚乙烯树脂为主要原料，添加必要的抗氧剂等助剂，经挤出加工而成的一种新型产品。广泛应用于厂房、住宅、宾馆、学校、商场、医院、办公等场所的集中供热与制冷的地源热泵系统。

管材规格范围dn25mm,dn32mm,dn40mm。压力范围1.0MPa-1.6MPa。

产品特点

- 内壁光滑，水流阻力小。

- 韧性、挠性好，对基础不均和错位的适应能力强。

- 耐腐蚀性强，用于输送含有防冻剂等腐蚀性介质时无需做防腐处理，使用寿命长。

- 导热性能优良，低温抗冲击性能好。

- 电熔（或热熔）连接方便可靠，施工和维护简便。

product introduction

HDPE pipe for geothermal heat pump system is a new type of product made of high-quality polyethylene resin as the main raw material, adding necessary antioxidants and other additives. Widely used in ground  geothermal  heat pump systems for central heating and cooling in factories, residences, hotels, schools, shopping malls, hospitals, offices and other places.

Pipe specification dn25mm-dn40mm. Pressure 1.0MPa-1.6MPa.

Features

1. The inner wall is smooth and the water flow resistance is small.

2. Good toughness and flexibility, strong adaptability to foundation unevenness and dislocation.

3. Strong corrosion resistance, no need for anti-corrosion treatment when used to transport corrosive media containing antifreeze, and long service life.

4. Excellent thermal conductivity, good impact resistance at low temperature.

5. The electric fusion (or hot fusion) connection is convenient and reliable, and the construction and maintenance are simple.

# PPR冷热水管

# PPR Pipe for Cold and Hot Water

产品简介

PPR管正式名为无规共聚聚丙烯管，是采用无规共聚聚丙烯经挤出成为管材，注塑成为管件，由于它使用无规共聚技术，使聚丙烯的强度，耐高温性得到很好的保证，是目前家装工程中采用最多的一种供水管道，广泛应用于建筑物内的冷热水管道系统，以及工业上的液体输送或化学介质排放等工业用途。

管材规格范围dn20-dn160mm。压力范围1.25MPa-2.5MPa。

产品特点

- 卫生性能可靠，无污染，属绿色建材。

- 耐腐蚀，正常使用寿命可达50年以上。

- 采用同质热熔连接，安装方便省时。

- 重量轻、强度高、韧性好，耐冲击性能良好。

- 产品内外壁光滑，流水阻力小，输送流体系统能耗少。

- 耐热能力高，长期正常使用工作温度为70℃，短时使用耐高温可达95℃。

product introduction

The official name of PPR pipe is random co-polymer polypropylene pipe, because it uses random copolymerization technology, the strength and high temperature resistance of polypropylene are well guaranteed,widely used in cold and hot water piping systems in buildings, and industrial purposes such as liquid transportation or chemical medium discharge in industry.

Pipe specification dn20-dn160mm. Pressure 1.25MPa-2.5MPa.

Features

1. Reliable hygienic performance, no pollution,green building material.

2. Corrosion resistance, the normal service life can reach more than 50 years.

3. Connection convenient and time-saving for installation.

4. Light weight, high strength, good toughness, good impact resistance.

5. The inner and outer walls are smooth, small flow resistance .

6. High heat resistance, the long-term normal working temperature is 70°C, and the short-term high temperature resistance can reach 95°C.

PE虹吸排水管

Siphon drainage PE Pipe

产品简介

虹吸式排水系统采用特殊设计的雨水斗，使雨水在很浅的天沟水深下即可在管道中形成满流状态。利用建筑物的高度和落水具有的势能，在管道中造成局部真空，使雨水斗及水平管内的水流获得附加的压力而形成虹吸现象。利用虹吸作用，加快积水在管道内的流速从而快速排净积水。避免雨水溢流、屋顶漏水甚至屋顶垮塌等事故，以保证人们正常的生产和生活。在虹吸排水系统中，使用最多的就是PE管。

管材规格范围dn32-dn315mm。管系列S12.5和S16两种。

product introduction

The siphon drainage system adopts a specially designed rainwater bucket, so that the rainwater can form a full flow state in the pipeline under a very shallow gutter depth. Using the height of the building and the potential energy of the falling water, a partial vacuum is created in the pipeline, so that the water flow in the rain bucket and the horizontal pipe obtains additional pressure to form a siphon phenomenon. The siphon effect is used to speed up the flow rate of accumulated water in the pipeline so as to quickly drain the accumulated water. Avoid accidents such as rainwater overflow, roof leakage and even roof collapse, so as to ensure people's normal production and life. In the siphon drainage system, the PE pipe is the most used.

Pipe specification dn32-dn315mm. Tube series S12.5 and S16 .

PE-RT地暖管

Polyethylene of Raised Temperature Resistance Pipe (PE-RT)

产品简介

PE-RT地暖的原料是一种采用特殊的分子设计和合成工艺生产的中密度聚乙烯，它采用乙烯和辛烯共聚的方法来提高PE管的耐热性，管材质量稳定可靠。适用于建筑冷热水管道系统、采暖系统。

管材规格范围dn20-dn32mm。压力范围1.25Mpa(S5),1.6Mpa(S4)。

产品特点

- 无毒、无味、 卫生性能好。

- 良好的稳定性和长期的耐压性能，使用寿命长。

- 重量轻，柔韧性能好，施工方便。

- 耐高温性能好，具有良好的抗热蠕变性能

- 耐低温、 抗冲击性能好，安全性高。

product introduction

The raw material of PE-RT floor heating is medium-density polyethylene produced by special molecular design and synthesis process. It adopts the method of copolymerization of ethylene and octene to improve the heat resistance of PE pipe, and the quality of the pipe is stable and reliable. It is suitable for building cold and hot water piping system and heating system.

Pipe specification dn20-dn32mm. Pressure 1.25Mpa(S5), 1.6Mpa(S4).

Features

1. Non-toxic, tasteless, good hygienic performance.

2. Good stability and long-term pressure resistance, long service life.

3. Light weight, good flexibility and convenient construction.

4. Good high temperature resistance and good thermal creep resistance.

5. Low temperature resistance, good impact resistance and high safety.

PE 通信子管

PE Casing Pipe

产品简介

PE 通信子管是以聚乙烯树脂为主要原料，经挤出成型的聚乙烯管材，其材质

坚韧、重量轻、强度高、抗冲击、耐腐蚀、内外表面光滑、磨擦系数小、穿缆容

易、施工效率高；电绝缘性能好，使用寿命长(地埋管寿命长达五十年)，经久耐

用，线路运行安全可靠；管段长、接头少、安装简便，管材可做成各种颜色，以示区分。适用于埋在地下，用作光纤电缆的保护，及城镇通信、电缆、有线电视网络线路护管及建筑物室内电缆的穿导、隔离与保护。

管材规格范围dn20-dn40mm。

product introduction

The PE communication sub-pipe is a polyethylene pipe extruded from polyethylene resin as the main raw material.Tough, light weight, high strength, impact resistance, corrosion resistance, smooth inner and outer surfaces, small friction coefficient, cable wear capacity easy, high construction efficiency; good electrical insulation performance, long service life (the service life of buried pipes is as long as 50 years), durable, safe and reliable; the pipe length is long, few joints, easy installation. The pipe can be made into various colors to show the distinction. It is suitable for buried underground to protect optical fiber cables, and the penetration, isolation and protection of urban communications, cables, television network line and indoor cables in buildings.

Pipe specification normally dn20-dn40mm.

PVC 穿线管

PVC Casing Pipe

产品简介

PVC 穿线管是阻燃绝缘 PVC 穿线管的简称，以聚氯乙烯树脂为主要原料，加入其他添加剂经挤出成型，用于 2000V以下工业与建筑工程中的电线电缆保护平直导管。其具有防潮耐腐蚀、阻燃绝缘、抗压性能优异、冷弯性能好等特点，连接简易，施工方便，被广泛使用于家庭室内装修和建筑工程水电安装等的穿管保护。

管材规格范围dn16-dn50mm。类型：中型，重型

product introduction

PVC casing pipe is the abbreviation of flame-retardant insulated PVC casing pipe. It uses polyvinyl chloride resin as the main raw material, and is extruded with other additives. It is used for protecting conduits for wires and cables in industrial and construction projects below 2000V. It has the characteristics of moisture resistance and corrosion resistance, flame retardant insulation, excellent compression resistance, good cold bending performance, etc., easy connection and convenient construction, and is widely used in pipe penetration protection for home interior decoration and construction engineering.

Pipe specification dn16-dn50mm. Type: Medium, Heavy

MPP电力管

MPP Power Cable Pipe

产品简介

MPP 电力电缆保护管，采用改性聚丙烯为主要原材料。具有抗高温、耐外压的特点，适用于 10KV 以上高压输电线电缆护套保护。MPP 管具有优良的电气绝缘性，强度高、抗冲击、抗蠕变等特点。可采用地下穿越的非开挖施工方式，广泛应用于市政、电力、电信、煤气、自来水、热力等管线工程；城乡非开挖水平定向钻进电力排管工程，及明开挖电力排管工程，城乡及工业废水排放等工程。

管材规格范围dn50-dn315mm。

产品特点

- 具有优良的电气绝缘性

- 具有较高的热变形温度和低温冲击性能

- 抗拉、抗压性能比HDPE高

- 质轻、光滑、摩擦阻力小，可热熔焊对接

- 长期使用温度-5~70°C

product introduction

MPP power cable protection pipe uses modified polypropylene as the main raw material. It has the characteristics of high temperature resistance and external pressure resistance, and is suitable for the protection of high-voltage transmission line cables above 10KV. MPP pipe has excellent electrical insulation, high strength, impact resistance, creep resistance and other characteristics. It can adopt the trenchless method of underground crossing, and is widely used in municipal, electric power, telecommunications, gas, tap water, heat and other pipeline projects; urban and rural non-excavation horizontal directional drilling power pipeline projects, and open excavation power pipeline projects , wastewater discharge and other projects.

Pipe specification dn50-dn315mm.

Features

1. Has excellent electrical insulation

2. High heat distortion temperature and low temperature impact performance

3. Higher tensile and compressive properties than HDPE

4. Lightweight, smooth, low frictional resistance.

5. Long-term use temperature -5~70°C

CPVC电力管

CPVC Power Cable Pipe

产品简介

CPVC（或PVC-C）埋地式高压电力电缆护套管以CPVC树脂为主要原料，加入抗冲剂，稳定剂等辅料经高速挤出而成的新型埋地式高压电力电缆保护套管。该产品具有强度高抗冲击、耐高温、耐高压、耐腐蚀、阻燃绝缘、使用寿命长、安装简便等特点。广泛用于城市电网，机场码头，工业园区，小区建设，交通路桥及城市路灯电缆敷设等工程。

管材规格范围dn50-dn250mm。

产品特点

1.内、外壁光滑平整，得于导线穿入。

2.耐热性能优良，能在93℃以上的环境下保持不变形。

3.阻燃绝缘，能经受3万伏以上的高压，使用会更安全。

4.强度高，环刚度可达10kpa，完全适用于各种道路的施工。

5.抗冲击，能经受1Kg重锤，2m高度的冲击力。

6.具有良好的阻燃性能，能离火即熄。

product introduction

CPVC (or PVC-C) power cable pipe is a new type of buried high-voltage power cable protective tube made of CPVC resin as the main raw material, adding anti-impact agent, stabilizer and other auxiliary materials through high-speed extrusion. The product has the characteristics of high strength, impact resistance, high temperature resistance, high pressure resistance, corrosion resistance, flame retardant insulation, long service life and easy installation. Widely used in urban power grids, airport terminals, industrial parks, community construction, traffic roads and bridges, and urban street lamp cable laying projects.

Pipe specification dn50-dn250mm.

Features

1. Inner and outer walls smooth, easy for wires to penetrate.

2. Excellent heat resistance and can maintain no deformation in an environment above 93°C.

3. Flame-retardant insulation, can withstand high voltage of more than 30,000 volts.

4. High strength, ring stiffness up to 10kpa, completely suitable for various road constructions.

5. Impact resistance, able to withstand the impact force of 1Kg heavy hammer and 2m height.

6. It has good flame retardant performance and can be extinguished immediately after leaving the fire.

PE 电力通信波纹管

PE Power and Telecom Corrugated Pipe

产品介绍

PE电力通信波纹管主要以HDPE（聚乙烯）为原料，适合温度范围较大 (-30°C~60°C)。 该管材因其独特的结构，外壁有凸起的波纹，内壁平滑，具有质量轻，抗冲击性能好，耐腐蚀性，耐寒耐热的优点，管材两头波谷中嵌有密封胶圈，具有很好的防水密封性，该产品广泛用于通讯，电线，电缆的铺设。

管材规格范围dn16-dn160mm。

product description

PE corrugated pipe is mainly made of HDPE (polyethylene) and is suitable for a wide temperature range (-30°C~60°C). Due to its unique structure, the pipe has raised corrugations on the outer wall and smooth inner wall. It has the advantages of light weight, good impact resistance, corrosion resistance, cold resistance and heat resistance. Sealing rubber rings are embedded in the troughs at both ends of the pipe. Excellent waterproof sealing, the product is widely used in communication, wire, cable laying.

Pipe specification dn16-dn160mm.

PVC格栅管

PVC Grid Pipe for Casing

产品介绍

PVC格栅管采用了优质聚氯乙烯树脂为主要原料，添加必要的助剂混合后，经过高速挤出后成型的多孔管材。其采用栅格状的力学结构，多孔一体，结构紧凑合理，受力均匀、抗压能力强。内壁光滑，穿线省力，具有良好的耐低温性及可绕性。增加预留管孔，提高通信孔位的利用率，提高工效、安装方便、降低工程造价等优点，广泛用于光纤通迅、有线电视、多媒体传输等工程。

管材规格：单孔，3孔，4孔，5孔，6孔，7孔，9孔

product description

The PVC grid pipe uses high-quality polyvinyl chloride resin as the main raw material, and after adding necessary additives and mixing, it is a porous pipe formed after high-speed extrusion. It adopts a grid-like mechanical structure, porous and integrated, reasonable structure, uniform force, and strong compression resistance. The inner wall is smooth,easy casing and labor-saving, and it has good low temperature resistance and wind-ability. It has the advantages of increasing reserved pipe holes, improving the utilization rate of communication holes, improving work efficiency, convenient installation, and reducing project cost. It is widely used in optical fiber communication, cable TV, multimedia transmission and other projects.

Pipe specification: 1 hole, 3 holes,4 holes, 5 holes, 6 holes, 7 holes, 9 holes

PE 梅花管

- PE Plum Blossom Pipe for Casing

产品介绍：

PE多孔梅花管是以高密度聚乙烯(HDPE）为原料，经挤出机一次挤出成型，各单孔壁相交，紧密熔接的一种线缆护套管材。具有刚柔兼备、抗冲击、耐腐蚀、使用寿命长、施工方便、工程造价低等优点。 主要用于通信电缆、电信光缆网络、长途通讯线路及有线电视广播传输网络等。

管材规格：5孔，7孔，9孔

特点：

1、耐腐蚀性强、电绝缘性好；

2、多孔分隔清晰，穿线轻松、方便；

3、一管多孔、施工方便快捷，工程造价低；

4、产品一体化结构，强度高，使用寿命长。

product description:

PE Plum Blossom Pipe is made of high-density polyethylene (HDPE), which is extruded by an extruder, and the walls of each single hole intersect and are tightly welded as a cable sheath pipe. It has the advantages of both rigidity and flexibility, impact resistance, corrosion resistance, long service life,convenient construction, and low engineering cost. It is mainly used in communication cables, telecommunication optical cable networks, long-distance communication lines and cable television broadcasting transmission networks, etc.

Pipe specification: 5 holes, 7 holes, 9 holes

Features:

1. Corrosion resistance and good electrical insulation;

2. The porous separation is clear, casing is easy and convenient;

3. Convenient and fast in construction, and low in construction cost;

4. The integrated structure of the product has high strength and long service life.

PE 硅芯管

PE silicon core pipe

产品介绍

PE硅芯管是一种内壁带有硅胶质固体润滑层的复合管道。由三台塑料挤出机同步挤压复合，主要原材料为高密度聚乙烯(HDPE)，芯层为摩擦系数最低的固体润滑剂硅胶质。密封性能好，耐化学腐蚀，工程造价低。广泛运用于通讯光纤、光缆、电缆等光电缆通信网络系统。

管材规格：dn32-dn63

产品特点

- 内壁滑润，永不脱落，摩擦系数极小；

- 曲率半径小，适应复杂的地理环境；

- 电绝缘性能好，使用寿命长（地埋管50年）。

- 抗压力强，施工便捷，维护费用低。

- 色底和彩条可定制；

- product description

- PE silicon core pipe，i.e.permanently lubricant high-density Polyethylene (PLB HDPE) duct,is a composite pipe with a silicone solid lubricating layer on the inner wall. Synchronously extruded and compounded by three plastic extruders, the main raw material is high-density polyethylene(HDPE), and the core layer is solid lubricant silica gel with the lowest friction coefficient. Good sealing performance, chemical corrosion resistance, low engineering cost. It is widely used in optical cable communication network systems such as communication optical fiber, optical cable, and electric cable.

- Pipe specification: dn32-dn63

- Features

- 1. The inner wall is smooth, never falls off, and the friction coefficient is extremely small;

- 2. Small radius of curvature, suitable for complex geographical environment;

- 3. Good electrical insulation performance and long service life (50 years for buried).

- 4. Strong pressure resistance, convenient construction and low maintenance cost.

- 5. Color base and color bar can be customized;

PE碳素螺纹管

PE Spiral Corrugated Pipe

PE碳素波纹管是采用高密度聚乙烯 (HDPE）与碳素复合材料旋转挤出成型工艺术生产的新型电力线缆保护管道。特殊的螺纹状造型，使其具有高强度、高韧性、耐腐蚀、 耐高温、绝缘电阻高、阻燃性好、质量轻、寿命长、不易变形等优点。广泛应用于城市路灯线路地埋工程，高速公路电力、通信设施的建设与改造工程，住宅小区建设工程及公园和大型娱乐场所的地埋电缆工程。

管材规格范围dn50-dn250mm。

HDPE Spiral Corrugated Pipe is a new type of power cable protection pipe produced by high-density polyethylene (HDPE) and carbon composite material rotary extrusion molding technology. The special thread shape makes it have the advantages of high strength, high toughness, corrosion resistance, high temperature resistance, high insulation resistance, good flame retardancy, light weight, long life, and not easy to deform. It is widely used in buried projects of urban street lamp lines, construction and renovation projects of expressway power and communication facilities, construction projects of residential quarters and buried cable projects in parks and large entertainment venues.

Pipe specification : dn50-dn250mm.

共三大类：20种

- 钢骨架聚乙烯（PE）塑料复合管

- Steel Reinforced  Polyethylene Plastic Pipe (SRPE)

- 产品介绍

- HDPE钢骨架管通过钢网焊接与塑料挤出同步进行，管壁的内外层塑料通过管壁中间的金属网孔连接为一体，钢丝与塑料间无明显界面，总体结构类似于钢筋混凝土，两种材料完全复合为一体，管材各部分质量均一、稳定。它克服了钢管耐压不耐腐，纯塑料管耐腐不耐压的缺点，既可像金属管道一样承压较高压力，又可像塑料管一样耐受各种化学物质侵蚀，是传统中低压管道的理想替代产品。产品广泛应用于石油化工、冶金矿山、电力、机场港口、市政燃气、给排水等行业。

- 产品特点

- 良好的韧性，结构类似钢筋混凝土, 刚柔相济

- 抗蠕变性能好，有效约束塑料的蠕变，持久机械强度高

- 抗腐蚀性能好，耐各种化学介质腐蚀，全面防腐耐高压

- 热膨胀系数小，结构优异耐高温，工作温度可达80℃

- 抗磨损性能高，内壁光滑，输送阻力小

- 耐冲击性能高，可抗快速开裂

- 使用寿命长，正常使用寿命可达50年以上

- 自示踪性好，方便检修

- 施工方便、连接牢靠

- 卫生环保，无污染

product description

SRPE pipe is synchronously manufactured with steel mesh welded and plastic extruded together. The inner and outer layers of plastic are connected together through metal mesh holes in the middle of the pipe wall. There is not obvious interface between steel wire and plastic, and the overall structure is similar to reinforced concrete. The two materials are completely composite into a integrated unit, it overcomes the shortcomings of steel pipes that are not resistant to corrosion, as well as plastic pipes that are not resistant to pressure, making it an ideal substitute for traditional medium and low pressure pipelines. The product is widely used in industries such as petrochemicals, metallurgy and mining, electricity, airports and ports, municipal gas, and water supply and drainage systems.

Features

- 1. High toughness, with a balance of rigidity and flexibility

- 2. High creep resistance, has high persistent mechanical strength

- 3.High corrosion resistance, resistant to various chemical media corrosion,

- 4. Low coefficient of thermal expansion, with a working temperature of up to 80 ℃

- 5. High wear resistance, smooth inner wall, and low conveying resistance

- 6. High impact resistance and resistance to rapid cracking

- 7. Long service life, with a normal service life of over 50 years

- 8. Good self tracking performance, convenient for maintenance

- 9. Convenient construction and reliable connection

- 10. Health and environmental protection, pollution-free